FOUNDRY GRADE SILICA SAND High Performance · Strong Molds · Defect-Free Castings

High-performance silica sand designed for strong molds, high permeability, and defect-free castings.

KEY FEATURES

| ✓ SiO₂ ≥ 98.5% | ✓ Wide AFS Range (25–100) | ✓ Low Clay & Moisture | ✓ High Permeability | ✓ Superior Bonding & Finish |
| --- | --- | --- | --- | --- |

TECHNICAL SPECIFICATIONS

| Parameter | Specification |
| --- | --- |
| SiO₂ | ≥ 98.5% |
| AFS Grain Fineness | AFS 25–30 · AFS 30–35 · AFS 35–40 · AFS 40–45 · AFS 45–50 AFS 50–55 · AFS 55–60 · AFS 60–65 · AFS 65–70 · AFS 70–75 & other grades available as per customer requirements |
| Clay | ≤ 0.20% |
| Moisture | ≤ 0.30% (Customizable) |
| Grain Shape | Sub-angular to Rounded |
| Permeability | High |
| LOI | ≤ 0.50% |
| Processing | Washed, Dried & Sieved |

END-USE APPLICATIONS

| Ferrous Foundries | Non-Ferrous Foundries |
| --- | --- |

TRUSTED BY INDUSTRY LEADERS

Our foundry sand is the preferred choice of some of India's most demanding manufacturers:

| SAIL | BHEL | Texmaco Rail |
| --- | --- | --- |
| Sonalika | Titagarh Rail Systems | Kiswok |

& many more across ferrous and non-ferrous sectors.

Note: AFS grain fineness numbers and moisture levels are fully customizable to meet specific casting and mold requirements. Please contact QMDC for tailored grades and bulk supply enquiries.