GLASS GRADE SILICA SAND Premium Quality · High Purity · Engineered for Optical Clarity

Low-iron, high-purity silica sand engineered for superior optical clarity and melting efficiency.

KEY FEATURES

| ✓ SiO₂ ≥ 99.0% | ✓ Ultra-Low Fe₂O₃ | ✓ Uniform Particle Distribution | ✓ Washed & Dried Processing | ✓ Customizable Grain & Moisture |
| --- | --- | --- | --- | --- |

TECHNICAL SPECIFICATIONS

| Parameter | Specification |
| --- | --- |
| SiO₂ | ≥ 99.0% |
| Al₂O₃ | ≤ 0.50% |
| Fe₂O₃ | Flint < 0.03% ¦ Amber / Green ≥ 0.11% |
| Moisture | ≤ 0.30% (Customizable) |
| Clay | ≤ 0.20% |
| Grain Size | 0.1 mm – 1.00 mm (Customizable) |
| Grain Shape | Sub-angular to Rounded |
| Color | White / Off-white |
| Processing | Washed & Dried |

END-USE APPLICATIONS

| Float Glass | Container Glass | Solar Glass |
| --- | --- | --- |

TRUSTED BY INDUSTRY LEADERS

Our silica sand is the preferred choice of major glass manufacturers across India, including:

Hindusthan National Glass (HNG)   ·   Gold Plus Glass   ·   & other leading manufacturers

Note: Grain size and moisture levels are customizable to suit specific manufacturing requirements. Please contact QMDC for tailored grades and bulk supply enquiries.